## Slide 1: SRF Results and Requirements
Internal MLC Review

## Slide 2: MLC Requirements
Cavities: SRF performance
  16.2 MV/m (13 MV) average (5GeV from 384 cavities)
  20 MV/m max (16 MeV) for overhead
  Q0 = 2*1010 on average at 16.2 MV/m (~11 W per cavity)
  Field stability (assuming non-correlated errors):
    Relative amplitude
      Baseline (1 sigma): 10-4
      Allowable (1 sigma): 6*10-3
    Phase
      Baseline (1 sigma): 0.1 deg
      Allowable (1 sigma): 1 deg

## Slide 3: Beamline: SRF Cavity
Parameter | Value
Accelerating mode | TM010 
Fundamental frequency | 1300 MHz
Design gradient | 16.2 MV/m
Intrinsic quality factor | >21010
Loaded quality factor | 6.5107
Cavity half bandwidth at QL= 6.5107 | 10 Hz
Operating temperature | 1.8K
Number of cells | 7
Active length | 0.81 m
Cell-to-cell coupling (fundamental mode) | 2.2%
Iris diameter center cell / end cells | 36 mm / 36 mm
Beam tube diameter | 110 mm
Geometry factor (fundamental mode) | 270.7 Ohm
R/Q (fundamental mode) | 387 Ohm
Epeak/Eacc (fundamental mode) | 2.06
Hpeak/Eacc (fundamental mode) | 41.96 Oe/(MV/m)
f/L | 1.6 kHz/mm
Lorentz-force detuning constant | ~1.5 Hz / (MV/m)^2
Cavity longitudinal loss factor for σ=0.6mm, non-fundamental | 13.1 V/pC
Cavity transverse loss factor for σ=0.6mm | 13.7 V/pC/m
 | Static Heat Load | Dynamic Load
2 K | <1 W | 11 W/cavity

## Slide 4: Prototype Cavity Fabrication
Quality control: CMM and frequency check
Electron Beam Welding
Finished main linac cavity with very tight (±0.25 mm) shape precision  important for supporting high currents (avoid risk of trapped HOMs!)
Notes: Mention CMM!

## Slide 5: One-Cavity ERL Main Linac Test Cryomodule
cavity
HOM load
HOM load
HGRP
80K shield
Gate valve
Assembled and currently under testing at Cornell:
  First full main linac system test
  Focus on cavity performance and cryogenic performance

## Slide 6: Test Results of First ERL Main Linac Cavity in Test Cryomodule
Cavity surface was prepared for high Q0 while keeping it as simple as possible: bulk BCP, 650C outgassing, final BCP, 120C bake
The achievement of high Q is relevant not only to Cornell's ERL but also to Project-X at Fermilab, to the Next Generation Light Source, to Electron-Ion colliders, spallation-neutron sources, and accelerator-driven nuclear reactors.
Administrative limit. Cavity can go to higher fields
Cavity exceeds ERL gradient and Q0 specifications: Q0=4 to 61010 at 1.6K in a cryomodule!

## Slide 7: High Q0 Results from Elsewhere
9-cell Cavity test in Horizontal Test Cryostat at HZB
Q0 > 2*1010 at 16 MV/m and 1.8 K
Average performance of eight 9-cell cavities in a FLASH cryomodule at DESY
1.6K
1.8K
2K
Q0 ~ 2*1010 at 16 MV/m and 1.8 K

## Slide 8: MLC Requirements
RF input coupler:
  5kW peak
  2 kW CW average
  Fixed coupling with Qext = 6.5*107
Superconducting quadrupole
  Maximum current: 110 A
  Maximum gradient: 19.4 T/m

## Slide 9: Beamline: Input Coupler
 | Static Heat Load | Dynamic Load at 2 kW CW
2 K | 0.03 W | 0.15 W
5 K | 1.55 W | 1.94 W
80 K | 2.26 W | 9.33 W
2 kW average RF power
5 kW peak RF power
Fixed coupling
Large transverse flexibility (1 – 2 cm offsets)
5K and 40 – 80 K intercepts
Prototype tested successfully to full power

## Slide 10: Superconducting Magnet
One superconducting quadrupole
X-Y dipoles
Cooled at 1.8 K

## Slide 11: MLC Requirements
Beam and HOM damping:
  Maximum beam current: 2 * 100 mA (ERL mode)
  Bunch charge: 77 pC
  Bunch length: 0.6 mm (2 ps)
  Longitudinal loss factor of cavity: 13.1 V/pC
  Average HOM power per cavity: 200 W
  Peak HOM power per cavity: >400 W
  Average HOM power per module: ~1.4 kW

## Slide 12: HOM Beamline Absorber
5K intercept
40 to 80K intercept
SiC absorber ring brazed to metal ring
Shielded bellow
Flange for disassembly
Flange to cavity
HOM beamline absorber at ~80K
Includes bellow sections
Concept based on first generation ERL HOM load, but greatly simplified
Graphite loaded SiC gives effective, broadband absorber ( ~ 50 – i25)
Prototype fabricated and test successfully

## Slide 13: Beam-Break-Up simulations
Optimized cavity with 0.25 mm shape imperfections supports ERL beam currents well above 100 mA!
Note: includes realistic fabrication errors and HOM damping materials!
1mm
0.125mm
0.5mm
0.25mm

## Slide 14: MLC Requirements
Frequency tuner and microphonics:
  Slow tuner range: ~500 kHz
  Fast tuner range: >1 kHz
  Peak microphonics detuning: <20 Hz
    Sigma ~ 3.3 to 4 Hz (assuming peak = 5 to 6 sigma)
    Peak detuning counts (determines maximum RF power)!
      5 kW sufficient for 16.2 MV/m and 20 Hz detuning

## Slide 15: Frequency Tuner and Magnet
Includes slow and fast tuner
Prototype tested successfully with prototype main linac cavity in test cryomodule
  Excellent linearity and very small hysteresis with >400 kHz slow tuning range
  2 kHz piezo tuning range

## Slide 16: Microphonics Results From the HTC and Elsewhere
cavity
HOM load
HOM load
HGRP
80K shield
Gate valve
Sigma = 4.6 Hz
Peak = 18 Hz

## Slide 17: MLC Requirements
Alignment (from PDDR):
  Cavities:
    Transverse offset (x,y)
      Baseline (1 sigma): 0.5 mm
      Allowable (1 sigma): 2 mm
    Pitch
      Baseline (1 sigma): 1 mrad (0.8 mm over length of cavity)
      Allowable (1 sigma): 1.5 mrad (1.2 mm over length of cavity)
  Quadrupole
    Transverse offset (x,y)
      Baseline (1 sigma): 0.3 mm
      Allowable (1 sigma): 1.6 mm

## Slide 18: Alignment Results from the Injector Cryomodule using fixed Supports
ERL Injector Cooldown WPM Horizontal
-1.00
-0.50
0.00
0.50
1.00
4/29/08 0:00
4/30/08 0:00
5/1/08 0:00
5/2/08 0:00
Date-Time
X position [mm]
X1 [mm]
X3 [mm]
X4 [mm]
X5 [mm]
High precision supports on cavities, HOM loads, and HGRP for “self” alignment of beam line
  Rigid, stable support
  Shift of beamline during cool-down as predicted
Cavity string is aligned to 0.2 mm after cool-down!

## Slide 19
The End